## Slide 1
Power spectrograms recorded from multiple cortical regions reveal clear, stimulus-specific neural activity. Visual and somatosensory stimulations elicit distinct patterns in their corresponding cortical areas, with well-separated peaks and temporal dynamics that highlight the specificity and robustness of the recorded responses.
00
00
00
1Emotion, Cognition & Behavior Research Group, Korea Brain Research Institute (KBRI), Daegu 41062, Korea
2Department of Robotics and Mechatronics Engineering, Daegu Gyeongbuk Institute of Science and Technology (DGIST), Daegu, 42988, Republic of Korea
3Graduate School, Daegu Gyeongbuk Institute of Science & Technology (DGIST), Daegu, 42988 Republic of Korea
* Corresponding Email : nschou@kbri.re.kr
A Reconfigurable Multisite ECoG Array for Recording from Multiple Cortical Regions
Jimin Lee1.2†, Jonghee Eun1†, Juhyun Kim1*, Namsun Chou1,3*
Abstract
(a and b) Impedance and (d) cyclic voltammetry (CV) comparison between pristine and PEDOT-coated electrodes (c) SEM images comparing the surface morphology of electrodes with and without PEDOT:PSS (e) Aging test of electrodes for 4 weeks
Understanding distributed cortical dynamics requires simultaneous access to multiple brain regions. However, current approaches face significant limitations. Commercial ECoG electrodes typically require a large craniotomy to cover multiple areas, resulting in a highly invasive implantation procedure. Furthermore, MEMS-based ECoG arrays often demand extensive redesign to target different cortical area combinations, leading to increased fabrication time and complexity. Building upon the limitations of existing technologies, this work presents a reconfigurable multisite ECoG platform that offers significant advancements:
It targets diverse cortical areas through a single, less invasive implantation.
(2) It enables adjustable access by simply changing the packaging of the electrode array and the custom-designed PCB.
(3) This approach eliminates the need for redesign, overcoming the issues of increased fabrication time and complexity.
(4)Ultimately, it facilitates practical and versatile studies of large-scale neural processes in vivo.
(a, b) Time-series ECoG signals simultaneously recorded from the motor and visual cortex during rest, movement, and visual stimulation. (c, d) Visual evoked potentials (VEPs) during freezing and moving states.
(a) Illustration of VEP & SSEP experiments, (b) Time-series ECoG signals simultaneously recorded from the somatosensory and visual cortex during whisker and visual stimulation (c, d) VEPs and somatosensory evoked potentials (SEPs) during visual(light)-only and simultaneous visual + somatosensory(whisker) stimulation
Packaging & Implantation of ECoG Platform
The proposed ECoG platform successfully achieved stable, region-specific recordings of neural responses across multiple cortical areas in the mouse. Distinct visual-, motor-, and sensory-evoked activity was captured without cross-area signal crosstalk, demonstrating reliable spatial selectivity. These results validate the platform as a scalable and minimally invasive solution for systems-level neuroscience, enabling flexible cortical targeting solely through packaging orientation rather than redesigning the electrode itself. This unique reconfigurability supports efficient cortical mapping and high-throughput multimodal studies.
This work was supported by grants of the National Research Foundation (grant no.: NRF-2021R1C1C2011489) and Korea Brain Research Institute (grant no.: 25-BR-02-02, 25-BR-07-01) funded by the Ministry of Science and ICT of Korea.
Power spectrograms from multiple cortical regions showing distinct, stimulus-specific neural activity. Somatosensory (a), visual (b), and motor (c) stimulations evoke clear, region-specific response patterns.
a
b
c
a
b
c
d
e
e
d
(a) In-vivo implantation of the ECoG platform (b and c) Adjustable packaging between the ECoG array and the PCB, featuring a circular pad design for easily targeting multiple brain regions.
Schematic illustration of target regions (MC: motor cortex, VC: visual cortex, AC: Auditory cortex)and SSC: somatosensory cortex)
Surgical procedures
In vivo implantation
(a) Fixing the head in a stereotaxic frame
(b) Performing scalp and cranial incisions
(c) Positioning the ECoG electrode
(d) Fixing the device using dental cement
Electrochemical Characterizations
In vivo Recording-MC & VC
In vivo Recording-SSC & VC
Conclusion
Acknowledgement
stimulation(VC)
stimulation(VC)
c
d
SSC
VC
a
Whisker
Visual (light)
Visual
Whisker
b
Stimuli
a
b
c
somatosensory cortex
visual cortex
Motor cortex
SSC(L) & SSC(R)
SSC & VC
a
b
b'
c
c'
d
d'
Advanced NeuroTechnology Lab. https://sites.google.com/view/adv-neurotech-lab :